## Slide 1: Tensile strength and impact resistance properties of materials used in prosthetic check sockets, copolymer sockets, and definitive laminated sockets
Maria J. Gerschutz, PhD; Michael L. Haynes, MS; Derek M. Nixon, BS; James M. Colvin, MS

## Slide 2
Study Aim
  Evaluate tensile and impact properties of latest materials used to fabricate prosthetic check, copolymer, and definitive laminated sockets.
Relevance
  Although most prosthetic socket materials have been used for years, few are backed up by objective evaluations.
  Without knowledge of basic properties, trying new methods/materials risks violating long-forgotten lessons and patient safety.

## Slide 3: Comparisons Analyzed

## Slide 4: Selected Results
Raw specimens and fabricated specimens significantly differed for all prosthetic socket materials.
PETG = polyethylene terephthalate glycol.
Thermoplastic tensile strength
Copolymer: Impact resistance at 25.5 °C not reported because of incomplete breaks, suggesting influence of temperature.
Check socket materials: Only PETG was significantly affected by temperature.
Thermoplastic impact resistance

## Slide 5: Conclusions
Material properties determined in this study provide a foundation for understanding and improving quality of prosthetic sockets using current fabrication materials and a basis for evaluating future technologies.